## Slide 1: CoFe2O4
Co-ferrites (Fe3+ )[Co2+Fe3+]O4 are inverted spinels with ferrimagnetic structure.
Number of neighbours and distances (in Å) between the cations in tetrahedral and octahedral position.
Site types→ Neighbours ↓ | A-sites |  | B-sites | 
First nearest-neighbours | A-type | B-type | A-type | B-type
 | 4 / 3.63 | 12 / 3.47 | 6 / 3.47 | 6 / 2.96
Second nearest- neighbours | A-type | B-type | A-type | B-type
 | 12 / 5.93 | 16 / 5.44 | 8 / 5.44 | 12 / 5.13
Third nearest-neighbours | A-type | B-type | A-type | B-type
 | 12 / 6.95 | 12 / 6.87 | 12 / 6.63 | 12 / 5.93